| Product | Seal Coating | Color Primer | Main Material Paint | Top Coating |
| --- | --- | --- | --- | --- |
| Engredients | Alkali resistant emulsion,Glycol, Assistant material,Water | Resin emulsion,Color paste.Titanium dioxide,Assistant material | Resin emulsion,Color pasta,Titanium dioxide,Protective gum,Assistant material&Water | Silicon a crylic-acid emulsion,Glycol, Coalescing agents,Wetting agent |
| Theoretical Coverage | 8-10㎡/kg | 6-7㎡/kg | 0.6-0.8㎡/kg(2mm dry membrane thickness) | 6-7㎡/kg |
| Drying Time | Tack-free=2h; hard drying=12h | Tack-free=4h; hard drying=12h | Tack-free=4h; hard drylng=48h | Tack-free=4h; hard drying=48h |
| Repainting Time | 12h(25℃,50%RH） | 12h(25℃,50%RH） | 48h(25℃,50%RH) | Finish |
| Color | Milk White | Refer to the specific color you need | Refer to the specific color you need | Milk White |
| Package | 6KG/Barrel | 8KG/Bamel | 20KG/Barrel | 8KG/Barrel |