Zhejiang SO-FINE Self Adhesive Products Co., Ltd

Technical data sheet

SF1865（SF9520） POLYMERIC ONE WAY VISION FILM

PRODUCT REVIEW:

Perforated white/black Polymeric PVC film, white gloss with black backing for use on even transparent substrates from glass. After printing on the film surface the picture becomes visible while the perforated black backing allows light to pass through.

APPLICATION：

For short and medium-term advertising graphics on vehicles, shop windows ,Airport graphics ,subway window, glass walls of building or other even surfaced transparent advertising media from glass that should allow light to easily pass through from back.

PRINTING METHOD:

Compatible with Solvent Ink, Eco-solvent, Latex, and UV Curable Inks.

TECHNICAL DATES:

| CHARACTERISTIC | TEST METHOD | AVERAGE VALUES |
| --- | --- | --- |
| Film thickness | ISO 4591:1992 | 160 ±10microns white/black Polymeric pvc film |
| Adhesive type |  | Solvent polyacrylate, removable ,transparent |
| Adhesive Removability |  | Within 1 year residueless removable from most surface |
| Release paper |  | Punched liner laminated with Double PE Coated Liner |
| Dimensional stability | FINAT TM14 | Adhered to glass, no shrinkage in cross direction, in length 0.5mm max |
| Temperature resistance |  | Adhered to glass. -20℃ to +65℃, no variation |
| Diameter of hole |  | 2.0 mm |
| Perforating ratio |  | 50% |
| Seawater resistance | DIN 50021 | Adhered to glass, after 48h/23℃ no variation |
| Adhesive power | FINAT TM1 | After 24h stainless steel 5±2N/25 mm |
| Tensile strength along across | DIN EN ISO 527 DIN EN ISO 527 | Min.5Mpa Min.5Mpa |
| Elongation at break along across | DIN EN ISO 527 DIN EN ISO 527 | Min50% Min50% |
| Shelf life |  | Up to2 years |
| Application temperature | Clean, dry surface | Min.+10℃ |
| Service life by specialist application | Under vertical outdoor exposure | Normal climate of china Up to 2 years |
| Attention: After printing the ink must be thoroughly dry in order to avoid any affect on the later combination with the laminate. Surfaces to which the material will be applied must be thoroughly cleaned from dust, grease or any contamination which could affect the adhesion of the material. The statements in this information sheet are based upon our knowledge and practical experience. This data is intended only as a source of information and is given without guarantee and does not constitute a warranty. Due to the wide variety of possible uses and applications customers should independently determine the suitability of this material for their specific purpose, prior to use. |