Specification

for LITHIUM BATTERY

锂电池技术规范

| approved by （批准） |  |
| --- | --- |
| Department （部门） |  |
| Name （姓名） |  |
| Title （标题） |  |
| signature/date （签名/日期） |  |

(Remarks: the above table shall be filled by customer 上表须由客户填写)

Issued by (拟制):  仪燕会

Checked by （复核）:  许杰康

Approved by （批准）:  夏青

Document number(文件编号) : WI-S-a5

Version number （版次）: A/0

DATE :  2021-01-01

YICHANG POWER GLORY TECHNOLOGY CO., LTD.

宜昌力佳科技有限公司

NO.19，XIANFENG ROAD，XIAOTING DISTRICT，YICHANG CITY，HUBEI PROVINCE，CHINA

中国湖北省宜昌市猇亭区先锋路19号

TEL:0717-6533688  6537588

FAX:0717-6523399  http://www.szlijia.com.

Lithium Manganese Dioxide Battery

Model   CR1616

Specifications

Nominal Discharge current          0.1mA

Nominal Voltage                          3V

Nominal Capacity                        50(mAh)

Continuous stangard  load           30(kΩ)

Maximum pluse current               8mA

Operating temperature                -20℃~70℃

Weight                                         1.2（g）

UL Recognition                           MH29853

## Characteristics

Manufacturers：YICHANG    POWER   GLORY  TECHNOLOGY  CO.,  LTD.

# ＜WARNING＞

# (1)Never charge the battery. Charging the battery may cause seethe of thebattery electrolyte or increase of the battery internal pressure. Leakage, heating, explosion or ignition of the battery may be caused as a result of it.

(2)Keep away from infants. If infant happens to swallow the battery, consult a doctor Immediately

(3)Note: if the temperature is higher than the continuous use + 60 ℃ or below -10℃. Please contact the Power Glory

Date of issue: Nov  2020

TEL:0717-6533688    0717- 6537588

FAX:0717-6523399     http://www.szlijia.com.

■Characteristics : [TABLE 1] TEST ITEMS TEMPERATURE INITIAL AFTER 12 MONTHS REMARKS Open-circuit Voltage 20±2℃ 3.0V TO 3.4V 3.0V TO 3.4V Closed-circuit Voltage 20±2℃ 3.0V TO 3.4V 3.0V TO 3.4V Standard Load Resistance . 0.8 Sec. [ TABLE 2 ] TEST ITEMS TEMPERATURE INITIAL AFTER 12 MONTHS REMARKS Service Life 20±2℃ See graph for details ≥ 98% of initial capacity Continuous Discharge Under Standard Load to 2.0V End-Voltage [ TABLE 3 ] TEST ITEM STORAGE TEMP STORAGE PERIOD REQUIREMENT REMARKS Service Life After Storage At High Temperature 60 ±2℃ 20 Days ≥ 98% of initial capacity Continuous Discharge At 20± 2℃Under Standard Load To 2.0V End-Voltage After Storage. [ TABLE 4 ] TEST ITEM REQUIREMENT TEST CONDITIONS Leakage Characteristics No Leakage Temperature: 45 ± 2℃, Relative Humidity: 75% Storage: 30 Days Shall Be Inspected By Visual Means [ TABLE 5 ] TEST ITEM REQUIREMENT TEST CONDITIONS Self-discharge 2% or Below Continuous Discharge Under Standard Load To 2.0V End-voltage After 12 Months Storage At 20℃. ( To Obtain From The Mean Value Of The Same Lot ) Markings:

■Markings:

Markings on batteries  :

5.1.1 Battery type :                       CR1616

5.1.2 Brand of battery:                 Omnergy

5.1.3 Polarity :                               + [(-) shall  not be indicated]

5.1.4 Manufacturing marks  : The year and month of production shall be

marked on the negative (-) terminal side

o  o P

P/H Type Month of production (1 letter) Year of production (The last number of Christian era)

[Example]  01P       P/H type Manufactured in January 2020

0XP      P/H type Manufactured in October 2020

0YP      P/H type Manufactured in November 2020

0ZP      P/H type Manufactured in December 2020

Month of production.

- January to September -- 1- 9

- Oct, Nov, Dec, -------X,Y, Z

■Precautions in Designing a Memory Backup Circuit

A primary lithium battery is not rechargeable.When used for memory backup in combination with another power source, current may flow into the battery from the other source. To prevent this, include a protection diode and resistor in the circuit so that no battery charging or over discharging can occur.Allowable Range of Diode Back-Leakage Current .To prevent the battery from being charged by the main power source, be sure to use a back-current prevention diode and a protection resistor. Select a silicon diode or a Schottky diode with minimum leakage current, and design the circuit so that the amount of charging due to leakage current does not exceed 1% of the nominal battery capacity over the total period of use.

■Maximum Allowable Charge Current to Battery

| Model | Maximum allowable charging current | Model | Maximum allowable charging current | Maximum allowable charging voltage |
| --- | --- | --- | --- | --- |
| CR1620 | 10mA | CR2430 | 10mA | 5V |
| CR1632 | 10mA | CR2450 | 15mA |  |
| CR2016 | 10mA | CR2477 | 15mA |  |
| CR2025 | 10mA | CR3032 | 15mA |  |
| CR2032 | 10mA | CR3832 | 15mA |  |
| CR2050 | 10mA |  |  |  |

Protection resistance R must exceed the value calculated in the following formula:

■Precautions for Mounting

1. Overlapping Batteries

Lithium Manganese Dioxide Battery is shaped as shown below. It has exposed positive(+)and negative(-) metallic surfaces with a thin cylindrical seal, called the gasket, inbetween them. When the batteries are overlapped or mixed together in a disorderly way, their positive(+)and negative(-)terminals touch each other, causing short-circuits.

2. The Batteries Put in a Metallic Container or on a Metallic Plate

Similar to the overlapping battery problem, when the batteries are put in a metallic container or on a metallic plate, their positive(+)and negative(-)terminals may short-circuit through the conductive surface, depending on how the batteries are position.

3. When The Battery is Held with Metallic Tweezers

When held with a pair of metallic tweezers as shown, the battery short-circuits through the tweezers.

- When The Battery Lead Plates Touch Each Other

When the battery lead plates bend and touch each other or other either terminal, the battery short-circuits.

5. older Bridges

Solder may bridge between circuit board conductors, causing a short-circuit and draining the battery.

6. Short-circuits through Soldering Irons

Similar to solder bridging, when the circuit board wiring is short-circuited by a soldering iron for an extended period the battery is drained and consumed. Complete short-circuits through soldering irons within 5 seconds.

- Short-circuits through Piled Circuit Boards

When circuit boards with the batteries are piled on top of one another, their conductive traces may touch and form a battery discharge circuit that consumes the battery's power.

8. Discharge through Conductive Electrostatic Prevention Mats

Conductive mats are widely used to prevent static electricity from destroying semiconductors. If a circuit board with mounted battery is put on a conductive mat, the soldered conductors may touch the mat,providing a discharge path for the battery.

9. Improper Battery Mounting Polarity

When the battery's positive (+)and negative (-)terminals are reversed with respect to the battery mounting's polarity marks, the battery may be discharged, depending on the type of electric circuit.

10. Solder

When the battery lead plates are dipped in a molten solder bath, the battery is temporarily short-circuited. Therefore, complete dipping within 5 seconds.

■Handling Precautions

Please read and observe the follwing precautions thoroughly.

Lithium Manganese Dioxide Battery contains flammable materials, such as organis solvent. Improper battery handling may cause leakage, heating, explosion or ignition of the battery, which may lead to injury or product failure.

■PRECAUTIONS

1.Do not put the battery into microwave over or drying machine.

2.Do not drop, apply excessive damage or deform the battery.

3.Do not mix the used battery together with the new battery or different type of batteries.

4.Do not store the battery in high temperature and high humidity location and where the battery is exposed to sunlight to avoid performance deterioration, swelling or leakage, of the battery.