TR透明鞋底与鞋垫材料

产品介绍

本产品透明度高，底色白度高，耐温高，弹性好，加工性能好，长久放置不变色。本产主要适用于EVA人字拖鞋内垫、时装休闲鞋鞋垫、男女内增高鞋垫、透明鞋底、透明手柄、吸盘、玩具、桌角、牙胶、婴儿玩具、鞋底组合装饰品等透明配件。

产品物性

| 型号 | 邵氏硬度 Shore A | 密度 g/cm3 | 外观 | 体积磨耗 mm3 | 拉伸强度 MPa | 断裂伸长率 % | 撕裂强度KN/m | 耐黄变等级 | 耐折 次数 | JAMES 干式止滑 | JAMES 湿式止滑 | 备注 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ISO 868 | ISO 1183 |  | ISO 4649 | ISO 527 | ISO 527 | ISO 34 | HG/T 3689 | GB/T 3903 | ASTM D 2047 | ASTM D 2047 |  |
| 1661 | 15~40 | 0.90~0.92 | 高透 | 150~170 | 8~10 | 1200~1300 | 35~37 | ----- | 5万次无龟裂 | 1.18 | 1.12 | SBS 系列 |
|  | 50~70 | 0.93~0.94 | 全透 | 120~145 | 12~18 | 1100~1150 | 34~35 | ----- |  | 1.12 | 1.08 |  |
| 1661A | 15~45 | 0.90~0.92 | 高透 | 145~170 | 8~11 | 1150~1300 | 35~38 | 4 | 5万次无龟裂 | 1.18 | 1.12 |  |
|  | 50~70 | 0.93~0.94 | 全透 | 120~140 | 13~19 | 1100~1150 | 34~35 | 4 |  | 1.12 | 1.08 |  |
| 1661B | 25 | 0.91 | 高透 | 135 | 12 | 1200 | 40 | ----- | 5万次无龟裂 | 1.18 | 1.12 |  |
| 1665 | 15~35 | 0.91~0.92 | 全透 | 135~160 | 9~19 | 1100~1200 | 36~40 | ----- | 5万次无龟裂 | 1.18 | 1.12 |  |
| 6600 | 10~12 | 0.90~0.95 | 半透 | ----- | 7~8 | 850~900 | 50~56 | ----- | 5万次无龟裂 | 1.12 | 1.09 | SEBS 系列 |
|  | 0~40 | 0.87~0.88 | 全透 | ----- | 5~18 | 600~1450 | 51~75 | ----- |  | 1.12 | 1.09 |  |

说明：以上数据为测试平均值，仅供参考

加工工艺

| 料筒各段温度 | 喂料段温度 ℃ | 中段温度 ℃ | 前段温度 ℃ | 喷嘴温度℃ | 模具温度 ℃ | 加工上限温度℃ | 注射速度 | 备注 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 典型加工温度 | 150 | 155 | 160 | 160 | 20 | 200 | 中速 | SBS系列 |
| 加工温度范围 | 150~200 | 150~200 | 150~200 | 150~200 | 20~40 |  |  |  |
| 典型加工温度 | 180 | 190 | 200 | 200 | 40 | 250 | 快速 | SEBS 系列 |
| 加工温度范围 | 160~240 | 160~240 | 160~240 | 160~240 | 20~60 |  |  |  |

说明：以上加工工艺数据仅供参考

产品特点

- 有橡胶的弹性、质感与观感

- 表面有光亮、高透明度

- 手感好、弹力足

- 不含有毒成分，完全合乎环保材料要求

- 易加工（可以直接车线）、可回收利用

TR Transparent Sole and Insole Materials

Product Introduction

Our TR products are high transparency, high whiteness on undercoat, high temperature resistance, and good processing properties, Keep it long, no discoloring. It mainly apply to transparent fittings such as EVA flip-flops inner pad, fashion leisure shoe insole, male/female higher shoe insole, transparent outsole, transparent handle, sucker, toys, table edge, gutta-percha, baby toys and outsole assemble fittings.

Grade and Properties

| Type | Durometer Hardness Shore A | Density, g/cm3 | Appearance | Abrasion Volume Loss, mm3 | Tensile Strength, MPa | Elongation at Break, % | Tear Strength, KN/m | Discoloration Rating | Flexing Resistance | JAMES Dry Slip Resistance | JAMES Wet Slip Resistance | Remark |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ISO 868 | ISO 1183 |  | ISO 4649 | ISO 527 | ISO 527 | ISO 34 | HG/T 3689 | GB/T 3903 | ASTM D 2047 | ASTM D 2047 |  |
| 1661 | 15~40 | 0.90~0.92 | High- Transparent | 150~170 | 8~10 | 1200~1300 | 35~37 | ----- | > 50,000 | 1.18 | 1.12 | SBS Serial |
|  | 50~70 | 0.93~0.94 | Full- Transparent | 120~145 | 12~18 | 1100~1150 | 34~35 | ----- |  | 1.12 | 1.08 |  |
| 1661A | 15~45 | 0.90~0.92 | High- Transparent | 145~170 | 8~11 | 1150~1300 | 35~38 | 4 | > 50,000 | 1.18 | 1.12 |  |
|  | 50~70 | 0.93~0.94 | Full- Transparent | 120~140 | 13~19 | 1100~1150 | 34~35 | 4 |  | 1.12 | 1.08 |  |
| 1661B | 25 | 0.91 | High- Transparent | 135 | 12 | 1200 | 40 | ----- | > 50,000 | 1.18 | 1.12 |  |
| 1665 | 15~35 | 0.91~0.92 | Full- Transparent | 135~160 | 9~19 | 1100~1200 | 36~40 | ----- | > 50,000 | 1.18 | 1.12 |  |
| 6600 | 10~12 | 0.90~0.95 | Semi- Transparent | ----- | 7~8 | 850~900 | 50~56 | ----- | > 50,000 | 1.12 | 1.09 | SEBS Serial |
|  | 0~40 | 0.87~0.88 | Full- Transparent | ----- | 5~18 | 600~1450 | 51~75 | ----- |  | 1.12 | 1.09 |  |

Postscript: Data shown are average values and should not de examined for specifications

Injection Molding Conditions

| Cylinder Temperatures | Feeding Zone ℃ | Centre Zone ℃ | Front Zone ℃ | Nozzle℃ | Mold ℃ | Maximum Processing Temperature ℃ | Injection Rate | Remark |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Recommended Temperatures | 150 | 155 | 160 | 160 | 20 | 200 | Moderate | SBS Serial |
| Processing Temperature Range | 150~200 | 150~200 | 150~200 | 150~200 | 20~40 |  |  |  |
| Recommended Temperatures | 180 | 190 | 200 | 200 | 40 | 250 | Fast | SEBS Serial |
| Processing Temperature Range | 160~240 | 160~240 | 160~240 | 160~240 | 20~60 |  |  |  |

Postscript: Data shown should not de examined for specifications

Product Characteristics

- Elasticity and appearance of the rubber

- Foggy and shinny surface

- Good feeling of touching and strong elasticity

- Free of toxic substances, meet the demand of environment protection

- Easy process, Sewing directly and recyclable