Jinan   Great  Material  Co.,  Ltd

Add:     44# Wen Hua Xi  Road ,Jinan City ,China

Tel: +86-531-8858 0380;           Fax:+86-531-8858 0380

Website:  www.jngreat.com   Mail: huamingweizhu@163.net

Glass Beads for Road Marking

The Glass beads are used for road marking paints and thermoplastic to provide excellent night retro-reflectivity .When the headlight shines on the road line ,the light is reflected by the glass beads ,and then the driver can drive the car in the correct way.

Usually ,the rate of glass beads in paint is 15%--25%,used for intermix and drop-on , we can produce all kinds of glass bead from 30um to 3000um,including uncoated glass bead ,coated glass bead with silicon or silane according to the AASHTO M247, BS6088, EN1423&1424, AS2009, and customer requirements.

Package: 25KG Plastic woven bag or 1000KG plastic woven bag.

The specific gravity:  2.4-2.6(g/cm3)

Refractive index:  1.5-1.6.

BS6088CLASS A (INTERMIX)

| Sieve(um) | Retained (%) |
| --- | --- |
| >1180 | 0--3 |
| 1180--850 | 5--20 |
| 850--425 | 65--95 |
| <425 | 0--10 |

(Roundness: 70% or better)

BS6088 GLASS B (DROP-ON)

| Diameter(um) | Retained (%) |
| --- | --- |
| >850 | 0--5 |
| 600--850 | 5--20 |
| 300--600 | 30--75 |
| 180--300 | 10--30 |
| <180 | 0--10 |

(Roundness: 80% or better)

Technical references
Appearance: Colourless and transparent ball, no visible bubbles and impurity.
Spherical beads: ≥80%(600< Sieve size< 850um，spherical beads≥75%)
Density:   2.4-2.6g/cm3
Refractive index: Nd≥1.50　
Glass bead composition:The glass bead is made of sodium and calcium. SiO2＞68%

Glass Beads for Blasting(Jetting)

The glass beads is suitable for high pressure sandblasting. Examples of usage are as follow :

1、To clean moulds in die-casting ,metal forging ,extrusion of glass , rubber and plastic .

2、To eliminate tensile steel increased fatigue resistance in turbine blads ,aircraft motor axle .

3、To debar flashing in electronic integrated circuit boards and frames and sealed plastic pipes .

4、To clear deposits in piston chambers .

5、To debar flashing in precision casting of metal tubes and non-ferrous metal parts .

| Itmes | Diameter(um) | Mesh Size |
| --- | --- | --- |
| 1 | 850--600 | 20--30 |
| 2 | 600--300 | 30--50 |
| 3 | 180--100 | 80--150 |
| 4 | 100--63 | 150--230 |

Technical references
Appearance: Clean and transparent, no visible bubbles and impurity.
Density:2.4-2.6g/cm3 
Hardness:6-7 
Spherical beads:≥75% 
SiO2 content:＞70%

Glass Bead for grinding

1)  Product Function
    With the advantages of smooth surface, even size, high hardness, wearable and stable, widely used as disperser, grinding media and filler materials in day, paint, ink and chemical industry. 
2)Product Specification:
Main products specification for grinding according to following table:

| No. | diameter(mm) | corresponding sieve size |
| --- | --- | --- |
| 1 | 1-2 | 18-10 |
| 2 | 2-3 | 10-8 |
| 3 | 3-4 | 8-6 |
| 4 | 4-5 | 6-4 |

You can choose different size glass bead between 1mm-5mm according to different function.

- Technical references
A: Appearance: Clean and transparent, no visible bubbles and impurity.
B: Specific gravity:2.4-2.6g/cm3
C: Hardness:6-7
D: Compressive strength:＞1200N

- Package:

1.Using double-deck package, the inner is polythene film and its thickness is not less than 0.5mm, the outer is plastic woven bag to prevent leak or damp. The net weight of each bag is 25±0.2kg. 
2.Using double-deck package, the inner is polythene film and its thickness is not less than 0.5mm, the outer is plastic wiven bag to prevent leak or damp. The net weight of each is 1000±8kg.
3.According to clients' requirement.