Product quality inspection certificate
Product name：Anionic polyacrylamide

Date of manufacture：002-2026.02.28 
The sample quantity：0.5KG
Test date: 2026.02.28 

Test results                         
	Test items
	
	Judgment basis
	Standard value
	Detection result
	Conclusion 

	Appearance
	
	GB17514-2017
	White powder
	qualified
	qualified

	Solid content mass fraction
	%
	GB17514-2017
	≥90
	92.40
	qualified

	Mass fraction of acrylamide monomer (dry group)
	%
	GB17514-2017
	≤0.05
	0.04
	qualified

	The molecular weight
	million 
	GB17514-2017
	≥16
	16.20
	qualified

	Dissolution time
	Min
	GB17514-2017
	≤90
	60
	qualified

	Insoluble residue
	%
	GB17514-2017
	≤0.2
	0.12
	qualified
	

	The purity
	%
	GB17514-2017
	≥99
	99.5
	qualified

	mesh number
	
	
	80-100
	
	


Test date：2026/02/28

inspector： 贺可可                                  reviewer： 郑磊    

                       Shenyang Runbang Environmental Technology Co., Ltd.
Quality Inspection Department

