Product quality inspection certificate

Product name：cationic polyacrylamide

date of manufacture：002-2025.12.29
The sample quantity：0.5KG
Test date: December29,2050
inspection result  

	Test items
	
	Judgment basis
	Standard value
	Detection result
	Conclusion 

	Appearance
	
	GB31246-2014
	White powder
	合格
	qualified

	Solid content mass fraction
	%
	GB31246-2014
	≥90
	92.40
	qualified

	Mass fraction of acrylamide monomer (dry group)
	%
	GB31246-2014
	≤0.05
	0.04
	qualified

	The molecular weight
	million
	GB31246-2014
	≥16
	16.20
	qualified

	Ion degrees
	%
	GB31246-2014
	
	
	

	Dissolution time
	Min
	GB31246-2014
	≤90
	60
	qualified

	Insoluble residue
	%
	GB31246-2014
	≤0.2
	0.12
	qualified
	

	The purity
	%
	GB31246-2014
	≥99
	99.5
	qualified

	Mesh number
	
	
	80-100
	
	


Test date：2025/12/29

inspector：   贺可可                             reviewer：  郑磊    

                         Shenyang Runbang Environmental Technology Co., Ltd.

Quality Inspection Department

