Flux cored wire
Name:Hard Welding flux cored wire
Model:HP100-O
Wire diameter:Φ2.8
Hardness(HRC):60-65

Properties and Uses: High chromium, high boron alloy tubular open arc wire.Suitable for low stress,low impact conditions of abrasive wear conditions.
Welding parameters: Welding current:200-400 Welding voltage:26-31
Precautions: Clear workpiece surfacing at the oil, rust, etc.; generally used for surfacing after machining workpieces not.
Delivery specifications: Ring fitted:50kg；Bottled:250kg

Name:Hard Welding flux cored wire
Model:HP200-O
Wire diameter:Φ2.8
Hardness(HRC):58-62

Properties and Uses: High-chromium alloy tubular open arc wire.Suitable for medium impact, high abrasion conditions under stress conditions.
Welding parameters: Welding current:200-400 Welding voltage:26-31
Precautions: Clear workpiece surfacing at the oil, rust, etc.; generally used for surfacing after machining workpieces not.
Delivery specifications: Ring fitted:50kg；Bottled:250kg

Name:Hard Welding flux cored wire
Model:HP300-O
Wire diameter:Φ2.8
Hardness(HRC):58-62

Properties and Uses: High chromium cast iron type open arc tubular wire.Suitable for high temperature fine abrasive, abrasive wear conditions of small shocks.
Welding parameters: Welding current:200-400 Welding voltage:26-31
Precautions: Clear workpiece surfacing at the oil, rust, etc.; generally used for surfacing after machining workpieces not.
Delivery specifications: Ring fitted:50kg；Bottled:250kg