Shenyang LongGreen S&T Co.,Ltd. Hotline : +86-024-25361668

No.108-2 Shenliao Road Shenyang China

Technical Data Sheet                                                                 LongGreen 7202

# Tire Inside Paint LongGreen 7202

Product Description: white emulsion，water based filler-free tire inside paint.

Mode of Action：

LongGreen 7202 is a water based filler-free tire inside paint. The product provides a very good slip of the bladder into the green tire and very effective release performance after cure. Furthermore it shows good air bleed. After the cure the inside of the tire is clean and smooth. The inner liner splice is not affected because the active ingredient does not show the negative separation effects normally observed  with  regular  silicon  oil.   Short  drying  time  and  low  consumption  make  the  product LongGreen 7202 very economical to use. The product does not give any stains or marks if accidently applied on the tire outside.

Key points in operation：

LongGreen 7202 is sprayed onto the inside of the tire blanks in an undiluted form or diluted form  using air atomizing spraying systems (recommended nozzle size: 0.5 – 1.0 mm). LongGreen 7202 has virtually no tendency towards sedimentation. However, gentle stirring is recommended during processing.

Application fields:

Tire industry.

Technical Data:

Composition: aqueous emulsion of high molecular silicone polymer and additives. Appearance: white emulsion.

Density: ~ 1.0g / cm3   (20℃)

Solids content： 11.8% ~14.0% （2h/105 oC）

PH :   6.0-8.0

Packing:

200 kg pack, plastic drum; 800 kg /pallet

50 kg pack, plastic drum; 450 kg / pallet

Safety and transport：

LongGreen 7202 is not classified  as a dangerous good  according to transport legislation,  so  we should transport it in term of  undangerous good. It has not any hurt if you use it in right way.

Storage：

LongGreen 7202 should be stored in cool and dry place with closed container. The product has a shelf life of 12 months in original closed containers at room temperature. The production date is stated on the labels of each container.

Do not allow to freeze.

Further information on storage conditions:

Keep  at  temperature  not  exceeding  35°C.  Do  not  allow  product  temperatures  to  go  below  a temperature of 5°C.

Further information:

Product technical  information and  data  is based  on the best  information  available and  does not constitute or imply a warranty or patent infringement of any kind. The user is responsible for testing product suitability prior to using into production.

version 1.0